Table II. Sock performance requirement

| Characteristic | Requirement | Test method |
| --- | --- | --- |
| Fiber analysis, percent 1/, 2/ |  |  |
| Wool (minimum) (see 3.2) | 52 | AATCC TM20 |
| Nylon (minimum) | 20 |  |
| Spandex (minimum) | 1 |  |
| Thickness, sole area (single ply), inch at 0.15 pounds per square inch (psi) | 0.16 to 0.20 | ASTM D1777 |
| Bursting strength, sock heel, pounds force (lbf) (minimum) | 85 | ASTM D6797 |
| Dimensional stability, percent (maximum) |  | See 3.5.1 |
| Length: foot and leg; each | 7 |  |
| Width: foot and calf; each | 7 |  |
| Elastic recovery, top cuff opening, percent after one hour (minimum) | 85 | See 3.5.2 |
| Graduated compression, millimeters of mercury (mmHg) |  |  |
| Graduated compression at ankle, average | 8 to 15 | See 3.5.3 |
| Graduated compression at calf, percent 3/ | 65 to 85 | See 3.5.3 |
| Vertical wicking, inches, after 30 minutes, after 3 launderings (minimum) | 2 | Launder per AATCC TM150, 1, IV, Ai, three cycles, where no detergent is added to the 3rd cycle (see 3.5.4). |

TABLE II. Sock performance requirements – Continued.

| Characteristic | Requirement |  | Test method |
| --- | --- | --- | --- |
| Colorfastness, rating (minimum) | All except black | Black |  |
| Laundering, accelerated |  |  | AATCC TM61, 1A, five cycles |
| Shade change | 4 | 3 | AATCC EP1 |
| Staining | 4 | 3 | AATCC EP2 |
| Perspiration |  |  | AATCC TM15 |
| Shade change | 4 | 3 | AATCC EP1 |
| Crocking, dry and wet | 4 | 3 | AATCC TM8 AATCC EP8 |
| Appearance after repeated launderings |  |  |  |
| Color change |  |  | Launder per AATCC 150, 1, IV, Ai, 25 and 50 cycles, where no detergent is added at each 5th cycle. Color change per AATCC EP9 |
| After 25 cycles (minimum) | Rating 4, no color streaking |  |  |
| After 50 cycles (minimum) | Rating 3, no color streaking |  |  |
| Pilling, rating (minimum) |  |  | ASTM D3512/D3512M |
| After 25 cycles (minimum) | 3 | 3 |  |
| After 50 cycles, (minimum) | 3 | 3 |  |
| FOOTNOTES: 1/ The final fiber content shall add up to 100 percent and consist of only wool, nylon, and spandex. 2/ Cotton and rayon shall not be used in the sock. 3/ Percent of the actual measured average ankle compression. 4/ Pilling testing shall be performed on the heel gore and toe sections only. |  |  |  |